	


GLASS BASALTIC CLOTH

Main technical standard
	 Woven fabric for industrial applications, made of 50/50% Glass and Basaltic yarn. 


[image: image1.jpg]



	 Property
	Standard/Method
	Unit
	Value

	Base material 

	Density of unsized filament 
	kg/dm³
	2,67

	Moisture content of basaltic rock 
	%
	0,1

	Melting point* 
	°C
	1350

	Fabric 

	Specific surface weight
	ISO 3374:2000
	g/m²
	940

	Weave type
	Twill 2/2

	Yarn density:

	- warp
	ends/cm
	3,8

	- weft
	ends/cm
	3,8

	Sizing type
	Silane

	°C
	-250°C – 550°C

	Breaking load:
	Calculated value

	- warp
	N/25mm
	>7600

	- weft
	N/25mm
	>7600

	Width
	ISO 5025:1997
	mm
	1270

	Thickness
	ISO 4603:1993
	mm
	0,53

	Moisture content (fabric)
	ISO 3344:1997
	%
	<0,3

	LOI, also sizing content
	ISO1887:1995
	%
	0,4-0,6

	Combustibility
	NF P92-503:1995
	M1
	Pass

	UV stability 
	ISO 105-B02
	>7


	Packaging

	Standard size 2mmx1mx20m (app. 28.66KG/ROLL) 


